Mimicking the Extracellular Matrix: Characteristics of Gelatin-Based, Cross-Linked Hydrogels for Potential Use in Treating Chronic Wounds

Ash Byrnes, Department of Biology, The College of Idaho, Caldwell, Idaho

Dr. Hu Yang (Advisor), Department of Biomedical Engineering, Virginia 	Commonwealth University, Richmond, Virginia

Dr. Scott Truksa (Advisor), Department of Chemistry, The College of Idaho, Caldwell, Idaho

Introduction:

The inflammatory response is a vital role of immune function and wound healing, in the case of a typical response known as acute inflammation. However, acute inflammation can develop into chronic inflammation. (Kumar et al. 2004). Chronic inflammation can last anywhere from months to years and is characterized by tissue necrosis at the wound site.

Tissue destruction is a key feature of chronic inflammation and is mainly caused by the release of matrix metalloproteinases (MMPs), which degrade the essential fibers of the extracellular matrix (ECM), such as collagen. This damage to the ECM creates extremely difficult problems when trying to repair tissue. (Jie et al. 2008). Without the ECM intact, healing wounds caused by chronic inflammation is improbable. Consequently, tissue must be regenerated in order to heal chronic wounds, such as pressure ulcers, commonly referred to as bed sores.

Although pressure ulcers and similar sores only occur in about 1-2% of the population, these wounds cost the U.S. Health Care System approximately $3.3 billion annually (Schwartz and Neumeister 2006). The majority of current treatments for pressure ulcers include debridement or the removal of necrotic tissue, turning the patient to relieve pressure, and use of dressings such as gauzes, hydrocolloids, and film with topical antibiotics and moisturizers. Although they are temporarily effective in decreasing infection and inflammation, these methods do not promote tissue regeneration and are therefore unlikely to promote wound healing. Additionally, current treatments show lack of patient comfort and compliance, further causing difficulties with treating and healing the wound, (Fonder et al. 2008).

The purpose of this project was to design and examine a different treatment method, using hydrogels and dendrimer-based drug delivery systems, in hopes of eventually promoting tissue regeneration in addition to combating infection. Additionally, this novel treatment was intended to increase patient comfort, ease of dressing application, and dressing durability. (Balogh et al. 2000).

Gelatin is a promising polymer for developing a hydrogel wound dressing as gelatin is collagen extract. Therefore, the hydrogel has the potential to mimic the extracellular matrix, which may lead to the tissue regeneration necessary for healing the wound (Balakrishnan et al. 2005). However, gelatin is water soluble, which could be problematic if the polymer is to function as a wound dressing. Therefore, the gelatin must be cross-linked or used with other polymers to maintain the dressing stability.  In this project, gelatin was electrospun with either polycapralactone (PCL) or nylon at a 1:1 weight ratio. In addition, half-generation (G3.5) polyamidoamine (PAMAM) dendrimers with encapsulated silver were loaded into nanofiber scaffolds and how the dendrimer-drug complex affected the physical characteristics of the dressing was determined. Silver was selected as the drug because it shows low toxicity in humans and binds strongly to enzymes used for respiration in microbes, making it an effective antimicrobial agent. (Balogh et al. 2000).

In this study the cross-linked gelatin scaffolds were tested in terms of permeability and average pore radius, water absorption, and mechanical strength. Permeability and pore radius of high values would facilitate cell migration and proliferation, which in turn, would increase the likelihood of tissue regeneration. Water absorption was also studied because pressure ulcers tend to secrete fluids and an absorbent dressing would help eliminate some of this exudate, hence decreasing frequency of dressing changes and increasing patient comfort. Mechanical strength tests were used to quantify the durability of the potential dressings. This study examined the differences between gelatin-based scaffolds cross-linked with PCL versus PGA as well as whether or not the presence of a dendrimer-based drug delivery system affected the scaffolds’ characteristics.

Goals for the summer: Unfortunately, due to unforeseen circumstances (the electrospinner in Dr. Bowlin’s lab breaking), I was unable to obtain the hydrogel scaffolds necessary to continue my studies over the academic year. However, since Dr. Yang’s laboratory is now using PGA instead of nylon as a copolymer due to its increased biodegradability, I am redoing everything I have done up to this point and expanding. Therefore, I will repeat the absorbance, permeability, and mechanical strength tests I did last year, as well as examining porosity, fiber diameter, and cellular interactions for PCL and PGA cross-linked scaffolds. I will also conjugate the tetracycline doxycylcine along with encapsulating silver within the dendrimer.

Protocol Outline:

Preparation of the dendrimer-doxycycline-silver complex – Use 10 mg of activated G3.5 PAMAM dendrimer to conjugate it with 15 mg doxycycline. Once the dendrimer has been conjugated, the silver will be encapsulated. Silver acetate is only somewhat soluble in water, so when silver acetate and the G3.5 PAMAM dendrimer were mixed in water, the silver encapsulated itself in the dendrimer, as this encapsulation process was energetically favorable. The preparation of dendrimer-silver complex will use 1 mL of deionized water and 12 mg of silver acetate (Balogh et al. 2000).

Preparation of the hydrogel – Gelatin, PCL, and PGA will be dissolved in hexafluoro-2-propanol overnight to have a concentration of 100 mg/mL before electrospinning. During this period, the solutions will be placed on a gentle vortex plate. Before electrospinning, the solutions will be prepared by mixing 2.5 mL of gelatin with either 2.5 mL of PCL or 2.5 mL of PGA for each scaffold. In one of the two gelatin/PCL mixtures and one of the two gelatin/PGA mixtures prepared, the dendrimer complex will added. All scaffolds will be spun at 22,000 volts at a rate of 4 mL/hour.

Permeability – The protocol and calculation for permeability will again be derived from Sell et al. 2008. Experiments are conducted at room temperature, distilled water used as the solvent, and the permeability device’s height is 1.5 m. Scaffolds will be punched into 21 mm diameter discs for the experiment.

Absorbance – Circular pieces of each scaffold (21 mm in diameter) will be used to measure adsorption and the mass of each piece obtained (WD). These pieces will then be placed in labeled centrifuge tubes filled with 1 mL of deionized water for twenty-four hours. The scaffold samples were then weighed again (WS). The following equation (from Balakrishnan et al. 2000) is used to calculate adsorption:

Mechanical Strength – Dog-bones will be punched from each of the scaffolds for use in the MTX Bionix 200 using Test Works 4 to calculate maximum stress and strain at breaking. Before measurements are taken, the thickness of each punch will be measured for input into Test Works 4 and the device calibrated. The dog-bones are placed on the MTX machine so that the thin, middle section of the punch was centered between the upper and lower clamps.

Porosity – Porosity will be measured by cutting 1 cm by 1 cm squares of the scaffold, measuring the thickness, and calculating volume. This will be compared to the known density of gelatin.

Fiber Diameter – Thirty points will be taken and calculated using Image Works.

Cell Studies – Still to be determined.

References:

Balakrishnan B, Mohanty M, Umashankar PR, Jayakrishnan A. 2005. Evaluation of an in situ forming hydrogel would dressing based on oxidized alginate and gelatin. Biomaterials 26: 6335-6342.

Balogh L, Swanson DR, Tomalia DA, Hagnauer GL, McManus AT. 2000. Dendrimer-Silver Complexes and Nanocomposites as Antimicrobial Agents. Nano Letters 1: 18-21.

Kumar V, Abbas AK, Fausto N. 2004. Robbins and Cotran Pathologic Basis of Disease. Philadelphia: W.B Saunders Company.

Fonder MA, Lazarus GS, Cowan DA, Aronson-Cook B, Kohli AR, and Mamelak AJ. 2008. Treating the chronic wound: A practical approach to the care of nonhealing wounds and wound care dressings. Journal of the American Academy of Dermatology 58: 185-206.

Jie L, Chen J, Kirsner R. 2007. Pathophysiology of Acute Wound Healing. Clinics in Dermatology 25: 9-18.

Microsoft Corporation. 2003. Microsoft Office Excel. Washington, USA.

MTS Systems Corporation. 2004. TestWorks4. Minnesota, USA.

Schwartz BF and Neumeister M. 2006. The Mechanics of Wound Healing. Future Directions in Surgery: 78-79.

Sell SA, Barnes C, Simpson D, Bowlin G. 2008. Scaffold Permeability as a Means to Determine Fiber Diameter and Pore Size of Electrospun Fibrogen. Journal of Biomaterials Research 85: 115-26.